Hygromorphic behaviour of cellular material: hysteretic swelling and shrinkage of wood probed by phase contrast X-ray tomography

D. Derome1, A. Rafsanjani1, 2, A. Patera1, 2, and J. Carmeliet1, 3

1Laboratory for Building Science and Technology, EMPA, Dübendorf, Switzerland

2Department of Civil, Environmental and Geomatic Engineering, ETH Zürich, Switzerland

3Chair of Building Physics, ETH Zürich, Switzerland

ABSTRACT:  Wood is a hygromorphic material, meaning it responds to changes in environmental humidity by changing its geometry. Its cellular biological structure swells during wetting and shrinks during drying. The origin of the moisture induced deformation lies at the sub-cellular scale. The cell wall can be considered a composite materials with stiff cellulose fibrils acting as reinforcement embedded in a hemicellulose/lignin matrix. The bulk of the cellulose fibrils, forming 50% of the cell wall, are oriented longitudinally, forming long-pitched helices. Both components of the cell wall matrix are displaying swelling. Moisture sorption and, to a lesser degree, swelling/shrinkage are known to be hysteretic.

We quantify the affine strains during the swelling and shrinkage using high resolution images obtained by phase constrast synchrotron X-ray tomography of wood samples of different porosities. The reversibility of the swelling/shrinkage is found for samples with controlled moisture sorption history. The deformation is more hysteretic for high than for low density samples. Swelling/shrinkage due to de/adsorption of water vapor displays also a non-affine component.

The reversibility of the swelling/shrinkage indicated that the material has a structural capacity to show a persistent cellular geometry for a given moisture state and a structural composition that allows for moisture-induced transitional states. A collection of qualitative observations of small subsets of cells during swelling/shrinkage is further studied by simulating the observed behavior. An anisotropic swelling coefficient of the cell wall is found to emerge and its origin is linked to the anisotropy of the cellulose fibrils arrangement in the cell wall layers.